Product Information Bulletin

451 - TWO PART POLYURETHANE FLOORING ADHESIVE

DESCRIPTION:

451 is a solvent-free, non-flammable, moisture and weather resistant two part polyurethane adhesive suitable for indoor and outdoor applications.  451 in particular, is suitable for adhering sheet vinyl and rubber floor-coverings in “wet” areas to most common interior and exterior sub-floors.  451 is also suitable for adhering vinyl plank and tile in areas where direct sunlight can affect the plank and tiles dimensions.

CHARACTERISTICS AND ADVANTAGES

451 Part A (Resin)					451 Part B (Hardener)

- Viscosity 		Paste				Liquid

- Colour		Grey 				Dark Brown

- Spec. Gravity	1.45kg/1			1.2kg/1

- Mixing Ratio	4.5 parts by weight		1 part by weight

- Pot life at 20(C	Approx. 60min , high temperatures accelerate, while low temperatures 					will retard curing.

- Coverage		1 - 3m( /Kg depending on condition of subfloor, trowel size used and 					floor-covering being used

- Curing		Minimum 8 hours - dependant upon ambient temperature and application. 					High Taffic areas minimum 48 hours, preferable.

- Resistance		Normal floor traffic acceptable after minimum 8 hours. 48 hours in high 					traffic areas.

- Resistance to

chemicals		Dilute acids, alkalis, solvents after 7 days.

SURFACES PREPARATION

All subfloor surfaces shall be dry, smooth, sound and clean, free of wax, grease, oil, old adhesive, paint, curing compounds, laitance, bond breakers and all other contaminants that inhibit adequate adhesion to the sub-floor.  The sub-floor must also be free from hydrostatic pressure or capillary action.  The adhesive should not be used in excessive cold or hot conditions i.e. below 8(c or above 28(c.

It is recommended that highly porous timer or concrete sub-floor surfaces be primed with Holdfast Uroseal and allowed to cure before applying the adhesive.

Timber sub-floors should be tested with an appropriate electrical resistance meter. The timber sub-floor should contain a maximum moisture content of 12%. Particle board flooring requires sanding to remove the wax sealer, prior to the use of this adhesive.  All concrete sub-floors should be tested for relative humidity (RH) prior to surface priming or application of adhesive. Ensure the RH (use insitu probe method ASTM F2170 current version) of the concrete sub-floor does not exceed 75%. Also ensure the surface pH of the concrete sub-floor is less than 9. Burnished concrete sub-floors must be ground back to allow for sufficient porosity and adhesion to the sub-floor.

If the sub-floor exceeds the recommended RH & pH  levels, sufficient remediation is required prior to the use of this adhesive.  All sub-floors should in accordance with current Australian Standard installation practices.

APPLICATION

1. Mix Part A (resin) with Part B (hardener). The quantities are at a ratio of 4.5 to 1 by weight. Stir the hardener thoroughly into the resin until a uniform grey colour is obtained (i.e. no streaks). For best results use a electric drill with mixing paddle attached. Maximum mixing time is 4 minutes.

2. Spread adhesive out onto a manageable area. Different trowel sizes will be needed for different floor-coverings.

3. Install the floor-covering into adhesive whilst still wet.

4. Roll the floor-covering per the manufacturer’s instructions.

5. Do not allow heavy traffic for 48 hours after installation of the floor-covering.

CLEAN UP

Remove excess adhesive while still wet with methylated spirits, tools must also be cleaned with methylated spirits before adhesive sets.

PRECAUTIONS

1. Do not use adhesive below 10(c or above 28(C of sub-floor conditions.

2. This product will not stand up to Hydrostatic pressure or capillary action.

3. Mixing procedure must be strictly followed as per our instructions.

4. Ensure gloves are worn when applying the polyurethane adhesive.

5. Do not allow adhesive to freeze, unaffected by freezing when dry.

# STORAGE AND USAGE

Use in well ventilated areas.  Keep container closed, store away from sources of heat. Do not allow adhesive to freeze, unaffected by freezing when dry.  This adhesive has a shelf life of 12 months from date of manufacture providing the adhesive is unopened and stored undercover at 20°C.

VENTILATION

Always make sure that there is adequate ventilation when using this adhesive.

CONDITIONS OF SALE:  contain a limited warranty against manufacturing defects.

# NOTICE TO THE PURCHASER

All statements and technical information contained herein are based on tests we believe to be reliable but the accuracy thereof is not guaranteed.  Users assume all risk and liability resulting from the use of this product and must confirm the suitability thereof by their own tests.

CONTACT POINT:		Technical Manager

TELEPHONE:		(03) 9797 1888

# Text boxes

September

2014